## Slide 1
Oil Charging
Addition Of Pentaerythritol
Addition of catalyst
Hold For MG formation
Check MG
Check Viscosity
Heat up to 150 °c
Alkyd Process Flow Diagram
Check samples for Viscosity, AV
Addition Of PA, Glycerine,MX
Cool and transfer to blender
Transfer to Tank through Filter
Heat up to 170 °c
Heat up to 260 °c
Heat gradually up to 230 °c
If Ok Cool up to 190 °c
If Not OK
After getting it ok
Add solvent
If OK
If Not OK

## Slide 2
N-Butanol charging
Addition Of Paraformaldehyde
Addition of catalyst
Hold For 4 hour
Check sample
Check Viscosity, Tolerance
UF Resin Process Flow Diagram
Add Urea
Addition Of Acid
Add Xylol
Cool the batch and pack into barrels through filter
Heat up to 105 °c
If Clear Cool up to 70 °c
If Not clear
Exothermic reaction
Heat gradually up to 116 °c
If OK
If Not OK
Check pH and if ok
Hold for 1 hr at 95 °c

## Slide 3
Phenol charging
Addition Of Catalyst
Addition of Paraformaldehyde
Hold at 55, 60, 70 & 80 °c
Check Viscosity
Add 2nd lot of butanol
Phenolic Resin Process Flow Diagram
Again add 1st part of butanol
Addition Of Butanol and Acid
Recover 1st lot butanol
Recover 2nd lot of butanol and cool the batch and pack into barrels after filtration
Exothermic Reaction
If Ok Cool up to 70 °c
If Not ok
Heat for distillation
Heat gradually up to 116 °c